SECTION 074213 – METAL WALL PANELS

This specification is applicable for IMETCO Cor-Pan exposed fastener wall panel system.

Delete the following instruction in RED Type.

IF YOU DO NOT SEE INSTRUCTIONS IN BLUE TYPE ABOVE THIS NOTE, PLEASE ACTIVATE HIDDEN TEXT AS INDICATED:

- Word 2010: File  Options  Display … Select “Hidden Text” from the “Always show these formatting marks on the screen” group.

- Word 2007: MS Office Button (top left of menu bar)Word Options (button in lower right of window)Display … select “Hidden Text”.

- Word 1997 - 2003: ToolsOptions … From the “View” tab, select “Hidden Text” from the “Formatting Marks” group.

- GENERAL

      - RELATED DOCUMENTS

- Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY.

- Modify as necessary

        - Work described in this section includes exposed fastener, lap-seam pre-formed metal wall panel system complete with fasteners, sealants, perimeter and penetration flashing and closures.

        - Related work specified elsewhere:

          - Structural steel.

          - Steel girts and furring.

          - Wood sheathing.

          - Rough carpentry.

          - Flashing and sheet metal. (Not wall panel related).

          - Air barrier and vapor retarder.

          - Thermal insulation.

          - Sealants.

      - DEFINITIONS

        - American Architectural Manufacturer Association (AAMA):

          - AAMA 621-96: Voluntary/Standard Specifications for High Performance Organic Coatings on Coil Coated Architectural Hot Dipped Galvanized (HDG) & Zinc-Aluminum Coated Steel Substrates

        - American Iron and Steel Institute (AISI):

          - S100-07: 2007 Edition of the North American Specification for the Design of Cold-Formed Steel Structural Members.

        - American Society of Civil Engineers (ASCE):

          - ASCE 7-05: Minimum Design Loads for Buildings and Other Structures.

        - American Society for Testing and Materials (ASTM):

          - A653-03: Specification for Steel Sheet, Zinc-coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process.

          - A755–03: Standard Specification for Steel Sheet, Metallic Coated by the Hot-Dip Process and Prepainted by the Coil-Coating Process for Exterior Exposed Building Products.

          - A792-03: Specification for Steel Sheet, 55% Aluminum-Zinc Alloy-Coated by the Hot-Dip Process.

          - B209-02a: Specification for Aluminum and Aluminum-Alloy Sheet and Plate.

          - D1056-00: Specification for Flexible Cellular Materials - Sponge or Expanded Rubber.

          - D3575-00e1: Standard Test Methods for Flexible Cellular Materials made from Olefin Polymers.

        - Sheet Metal and Air Conditioning Contractors National Association (SMACNA):

          - Architectural Sheet Metal Manual, 6th edition.

        - National Association of Architectural Metal Manufacturers (NAAMM)

          - Metal Finishes Manual for Architectural and Metal Products

      - DESIGN AND PERFORMANCE CRITERIA.

        - General Performance:  Metal wall panel assemblies shall comply with performance requirements without failure due to defective manufacture, fabrication, installation, or other defects in construction.

        - Thermal Expansion and Contraction.

          - Completed metal wall panel and flashing system shall be capable of withstanding expansion and contraction of components caused by changes in temperature without buckling, or reducing performance ability.

          - The design temperature differential shall be not less than 220 degrees Fahrenheit.

        - Uniform Wind Load Capacity.

          - Installed wall system shall withstand negative wind pressures complying with the following criteria.

            - Design Code: ASCE 7, Method 2 for Components and Cladding.

            - Safety Factor: 1.67.

- Select the negative wind pressure design factors that are applicable to this project. Please contact IMETCO for guidance in selecting appropriate factors and pressures for this specific project.

            - Category [I] [II] [III] [IV] Building with an Importance Factor of [0.77] [1.00] [1.15].

            - Wind Speed:       mph.

            - Exposure Category: [B] [C] [D]..

            - Height at Top of Wall System: ______ feet.

            - Minimum Building Width: ______ feet.

            - Roof Pitch (Above Wall System): ______ inches per foot.

- Wall Area	Negative Wind Pressure:

- Zone 4 - Field of Wall: 	+ ______ psf and - ______ psf.

- Zone 5 - Wall Edges: 	+ ______ psf and - ______ psf.

- The “a” dimension used to determine the width (measured from the corner of the building) of wall zone 5 shall be ______ feet.

          - The nominal capacity of the panel system shall be determined based on section property and strength of materials calculations in accordance with AISI S100. The allowable load carrying capacity shall be calculated by reducing the calculated nominal capacity by the safety factor listed herein.

      - SUBMITTALS.

        - Shop drawings: Show wall panel system with flashings and accessories in elevation, sections, and details. Include metal thicknesses and finishes, panel lengths, joining details, anchorage details, flashings and special fabrication provisions for termination and penetrations.  Indicate relationships with adjacent and interfacing work. Shop drawings to be prepared by metal wall panel manufacturer and sealed by a professional engineer registered in the state of the project location.

        - Financial Certification:  Provide the building owner with a signed and notarized (sealed) affidavit by an officer of the panel system manufacturer which confirms a current minimum corporate asset-to-liability ratio of not less than 3:1 for the panel manufacturer, or its parent corporation.  Financial support information and affidavit must be dated within 30 days prior to the product submittal.

        - Warranty: Provide unexecuted specimen warranty documents for each warranty as required in specification article 1.10.

        - Samples.

          - Submit sample of panel section, at least 6" x 6" showing seam profile with factory applied seam sealant, and also a sample of color selected.

          - Submit sample of panel clip and field applied sealants.

      - QUALITY CRITERIA/INSTALLER QUALIFICATIONS.

        - Engage an experienced metal wall panel contractor (erector) to install wall panel system who has a minimum of three (3) years experience specializing in the installation of metal wall systems.

        - Contractor must be certified by manufacturer specified as a supplier of the metal wall system and obtain written certification from manufacturer that installer is approved for installation of the specified system.

        - Successful contractor must obtain all components of wall system from a single manufacturer.  Any secondary products that are required which cannot be supplied by the specified manufacturer must be recommended and approved in writing by primary manufacturer prior to bidding.

        - Fabricator/Installer shall submit work experience and evidence of adequate financial responsibility.  Architect reserves the right to inspect fabrication facilities in determining qualifications.

      - DELIVERY, STORAGE, AND HANDLING.

        - Inspect materials upon delivery.

        - Handle materials to prevent damage.

        - Store materials off ground providing for drainage; under cover providing for air circulation; and protected from any debris.

      - PROJECT CONDITIONS

        - Weather Limitations:  Proceed with installation only when existing and forecasted weather conditions permit metal wall panel work to be performed according to manufacturer's written instructions and warranty requirements.

        - Field Measurements:  Verify actual dimensions of construction contiguous with metal wall panels by field measurements before fabrication.

      - COORDINATION

        - Coordinate sizes and locations of windows, doors, and wall penetrations with actual equipment provided.

- Modify the following paragraph to indicate the scope of this project.

        - Coordinate metal wall panels with rain drainage work, flashing, trim, and construction of other adjoining work to provide a leak proof, secure, and noncorrosive installation.

      - WARRANTIES

        - Endorse and forward to owner the following warranties:

          - Manufacturer's standard 20 year finish warranty covering checking, crazing, peeling, chalking, fading, and adhesion of the prepainted sheet metal materials.

          - Installer's 3 year warranty covering wall panel system installation and watertightness.

        - Warranties shall commence on date of substantial completion.

- PRODUCTS

      - PANEL MATERIALS

        - Painted, metallic-Coated Steel Sheet:  Restricted flatness steel sheet metallic coated by the hot-dip process and prepainted by the coil-coating process to comply with ASTM A755/A755M.

          - Recycled Content:  Provide steel sheet with average recycled content such that postconsumer recycled content plus one-half of preconsumer recycled content is at least 70 percent.

          - [24] [22] [20] gauge, Zinc-Coated (Galvanized) Steel Sheet, as per ASTM A653: G90 (Z275) coating designation; structural quality, grade 40 ksi (275 MPa).

- Stucco embossed material is generally NOT preferred for prefinished sheet steel materials. When specifying embossed material, there is always a risk of the process resulting in micro-fracture of the coating, which can lead to premature failure of the coating and corrosion of the substrate.

          - Texture:  [Smooth] [Stucco Embossed] surface.

          - Exposed Coil-Coated Finish:

            - 2-Coat Fluoropolymer:  AAMA 621.  Fluoropolymer finish containing not less than 70 percent PVDF resin by weight in color coat.  Manufacturers’ approved applicator to prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers’ written instructions.

            - Coating system shall provide nominal 1.0 mil (0.025 mm) dry film thickness, consisting of primer and color coat.

- Select one of the following 4 color choices:

            - Color shall be IMETCO’s ______.

            - Color shall be selected from IMETCO’s Standard Colors.

            - Color: Custom color selected by architect.

            - Color shall be: ______.

          - Concealed Finish:  Apply pretreatment and manufacturer's standard white or light-colored polyester backer finish, consisting of prime coat and wash coat with a minimum total dry film thickness of 0.5 mil (0.013 mm).

        - Clear acrylic coated, metallic-Coated Steel Sheet:  Restricted flatness steel sheet metallic coated by the hot-dip process and prepainted by the coil-coating process to comply with ASTM A755/A755M.

          - Recycled Content:  Provide steel sheet with average recycled content such that postconsumer recycled content plus one-half of preconsumer recycled content is at least 70 percent.

          - [24] [22] gauge, 55% Aluminum-Zinc alloy coated Steel Sheet, as per ASTM A792: AZ55 (AZ165) coating designation; with a nominal .04 mil (0.010 mm) dry film thickness of a clear organic polymer top film; structural quality, grade 50 ksi (340 MPa).

- Stucco embossed material is generally NOT preferred for coated sheet steel materials. When specifying embossed material, there is always a risk of the process resulting in micro-fracture of the coating, which can lead to premature failure of the coating and corrosion of the substrate.

          - Texture:  [Smooth] [Stucco Embossed] surface.

        - [Painted] [Mill Finish] Aluminum Sheet.

          - Recycle Content: Provide steel sheet with average recycled content such that postconsumer recycled content plus one-half of preconsumer recycled content is at least 45 percent.

          - [0.032”] [0.040”] [0.050”] aluminum alloy 3003, 3004, 3005, or 3105 with H14 or H24 heat treatment, as per ASTM B209/209M.

- Stucco embossed material is generally NOT preferred for prefinished aluminum sheet materials. When specifying embossed material, there is always a risk of the process resulting in micro-fracture of the coating, which can lead to premature failure of the coating and corrosion of the substrate.

          - Texture: [Smooth] [Stucco Embossed] surface.

- If Specifying Prefinished Painted Materials, Delete the following Section.

          - Mill Finish Aluminum: The exposed and unexposed sheet surfaces shall be bare as furnished by the mill.

- If Specifying Mill Finish Panels, Delete the following two Sections.

          - Exposed Coil-Coated Finish:

            - 2-Coat Fluoropolymer:  AAMA 621.  Fluoropolymer finish containing not less than 70 percent PVDF resin by weight in color coat.  Manufacturers’ approved applicator to prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers’ written instructions.

            - Coating system shall provide nominal 1.0 mil (0.025 mm) dry film thickness, consisting of primer and color coat.

- Select one of the following 4 color choices:

            - Color shall be IMETCO’s ______.

            - Color shall be selected from IMETCO’s Standard Colors

            - Color: Custom color selected by architect.

            - Color shall be: ______.

          - Concealed Finish:  Apply pretreatment and manufacturer's standard white or light-colored polyester backer finish, consisting of prime coat and wash coat with a minimum total dry film thickness of 0.5 mil (0.013 mm).

        - Panel Sealants:

          - Seam Sealant Tape:  Non-curing, 100 percent solids, polyisobutylene compound sealant tape with release-paper backing.  Provide permanently elastic, nonsag, nontoxic, nonstaining tape 1/2-inch- (13-mm-) wide and 1/8-inch- (3-mm-) thick.

          - Exposed Sealant:  ASTM C 920; elastomeric tripolymer, polyurethane, or other advanced polymer sealant; of type, grade, class, and use classifications required to seal joints in metal wall panels and remain weathertight; and as recommended in writing by metal wall panel manufacturer.

          - Concealed Sealant: ASTM C 1311: Butyl-Based, Solvent-Release, One-Part Sealant.

      - FIELD-INSTALLED THERMAL INSULATION

Delete this article if not required.  If retaining, indicate thicknesses on Drawings.

Retain first paragraph below and delete remainder of article if building insulation is included in Division 07 Section "Thermal Insulation."

        - Refer to Division 07 Section "Thermal Insulation."

        - Polyethylene Vapor Retarders: ASTM D 4397, 6 mils (0.15 mm) thick, with maximum permeance rating of 0.13 perm (7.5 ng/Pa x s x sq. m).

Retain one of first five paragraphs below.  Board insulation, which is typically installed over wall sheathing or fitted within cavity between liner and exterior panels, requires Z-shaped furring or channels to support metal wall panels.

        - Unfaced, Polyisocyanurate Board Insulation:  ASTM C 591, Type II, compressive strength of 35 psi (241 kPa), with maximum flame-spread index of 75 and smoke-developed index of 450.

        - Faced, Polyisocyanurate Board Insulation:  ASTM C 1289, [Type I (foil facing), Class 1 or 2] [Type II (asphalt felt or glass-fiber mat facing), Class 2 or 3, Grade 3], with maximum flame-spread index of 75 and smoke-developed index of 450, based on tests performed on unfaced core.

        - Extruded-Polystyrene Board Insulation:  ASTM C 578, Type IV, 1.60-lb/cu. ft. (26-kg/cu. m), with maximum flame-spread index of 75 and smoke-developed index of 450.

        - Molded-Polystyrene Board Insulation:  ASTM C 578, [Type I, 0.9 lb/cu. ft. (15 kg/cu. m)] [Type II, 1.35 lb/cu. ft. (22 kg/cu. m)], with maximum flame-spread index of 75 and smoke-developed index of 450.

        - Unfaced, Glass-Fiber Board Insulation:  ASTM C 612, Type IA or Types IA and IB; with maximum flame-spread index of 25 and smoke-developed index of 50, and with a nominal density of 3 lb/cu. ft. (48 kg/cu. m).

      - MISCELLANEOUS METAL FRAMING

        - Miscellaneous Metal Framing, General:  ASTM C 645, cold-formed metallic-coated steel sheet, ASTM A 653, G90 (Z275) hot-dip galvanized

Retain any of the paragraphs below as required.  Revise to suit Project.

        - Subgirts:  Manufacturer's standard C- or Z-shaped sections, 0.054-inch (16 gauge) (1.4-mm) nominal thickness.

        - Base or Sill [Angles] [Channels]: 0.068-inch (14 gauge) (1.7-mm) nominal thickness.

        - Hat-Shaped, Rigid Furring Channels:

          - Nominal Thickness:  As required to meet performance requirements

          - Depth:  [As indicated on drawings] [7/8 inch (22 mm)] [1-1/2 inches (38 mm)].

          - Top flange: 1-1/8 inches (28.5 mm) minimum

Retain first paragraph below for metal wall panels installed over unfaced board insulation.  Z-shaped furring is available in 1-, 1-1/2-, 2-, 2-1/2-, and 3-inch (25-, 38-, 51-, 64-, and 76-mm) depths.

        - Z-Shaped Furring:  With slotted or nonslotted web, face flange of 1-5/8 inches (41 mm) minimum and depth as required to fit insulation thickness indicated.

          - Nominal Thickness:  As required to meet performance requirements, but not less than 0.043 inch (18 gauge) (1.1 mm).

        - Fasteners for Miscellaneous Metal Framing:  Of type, material, size, corrosion resistance, holding power, and other properties required to fasten miscellaneous metal framing members to substrates.

      - SUBSTRATE BOARD

        - Glass-Mat Gypsum Sheathing Board:  ASTM C 1177/C 1177M.

          - Type and Thickness:  [Regular, 1/2 inch (13 mm)] [Type X, 5/8 inch (16 mm)].

- Retain the following paragraph is specifying a self-adhesive underlayment.

          - The top surface of the substrate board shall be pre-primed to provide for adhesion of the self-adhering underlayment material.

          - Product:  Subject to compliance with requirements, provide Dens Glass Gold by Georgia-Pacific Corporation.

        - Substrate-Board Fasteners:  Factory-coated steel fasteners and metal or plastic plates complying with corrosion-resistance provisions in FMG 4470, designed for fastening substrate board to structure.

      - UNDERLAYMENT MATERIALS

Underlayment materials should be selected with due consideration to the overall functions of the complete wall assembly. In most climate zones, impermeable membranes should be used on the interior side of the thermal insulating materials. On the exterior side of the thermal insulation, permeable (water-vapor open) membranes are generally required for adequate performance of the overall wall assembly. Please consult with IMETCO engineering for additional design recommendations.

        - Self-Adhering with reinforcing scrim, Vapor Impermeable, High-Temperature Sheet:  [50-mils- (1.3-mm-)] [60-mils- (1.5-mm-)] thick minimum, consisting of slip-resisting top surface laminated to SBS-modified asphalt adhesive, with release-paper backing; cold applied.

          - Thermal Stability:  Stable after testing at 250 deg F (121 deg C); ASTM D 1970.

          - Low-Temperature Flexibility:  Passes after testing at minus 20 deg F (29 deg C); ASTM D 1970.

          - Seams shall be lapped in accordance with manufacturer’s recommendations.

          - Underlayment shall be approved for 90 days (minimum) of exposure to UV and weather penetrations.

          - Products:  Subject to compliance with requirements, provide one of the following:

            - Aqua Block 50 by IMETCO of Norcross, GA.

            - Aqua Block 60 by IMETCO of Norcross, GA

            - Dry-Dek by IMETCO of Norcross, GA.

        - Self-Adhering, Vapor Permeable Sheet: 25-mils- (0.64-mm-) thick, minimum, consisting of a multi-layer polypropylene porous film laminate with a vapor permeable adhesive; cold applied.

          - Water Vapor Permeance, ASTM E 96 Method B: 50 perms (2,875 ng/(Pa*s*m2), minimum.

          - Water Resistance, AATCC 127, 22-inch- (550-mm-) hydrostatic head for 5 hours:  No leakage.

          - Seams shall be lapped in accordance with manufacturer’s recommendations.

          - Underlayment shall be approved for 120 days (minimum) of exposure to UV and weather penetrations.

        - Mechanically Attached, Vapor Permeable Sheet: 20-mils- (0.51-mm-) thick, minimum, consisting of multiple layers of UV stabilized spun-bonded polypropylene.

          - Water Vapor Permeance, ASTM E 96 Method B: 200 perms (11,500 ng/(Pa*s*m2), minimum.

          - Water Resistance, AATCC 127, 22-inch- (550-mm-) hydrostatic head for 5 hours:  No leakage.

          - Seams shall be lapped in accordance with manufacturer’s recommendations.

          - Fasteners:  Manufacturer's recommended corrosion-resistant, cap-headed steel or stainless steel nails, staples, or screws used in conjunction with manufacturer's spray adhesive, as appropriate for substrate.

          - Underlayment shall be approved for 270 days (minimum) of exposure to UV and weather penetrations.

      - MISCELLANEOUS MATERIALS

        - Concealed trim and flashing fasteners: Corrosion resistant steel screws, #10 minimum diameter x length appropriate for substrate, hex washer head or pancake head.  Use self-drilling, self-tapping for metal substrate or A-point for plywood substrate.

        - Exposed trim and flashing: Prepainted pan head or pancake head corrosion resistant coated or plated screws with neoprene sealing washer, or prepainted 1/8-inch- (3-mm-) diameter stainless steel rivets.

        - Exposed fasteners for anchorage of panels to wall framing: Corrosion resistant coated or plated carbon steel hex washer head screws with neoprene sealing washer, prepainted to match panels. Use #12 x 7/8” self-drilling, self-tapping for metal substrate or #14 x 1-1/2” A-point for wood substrate.

        - Exposed fasteners for stitching panel side laps: Corrosion resistant coated or plated carbon steel hex washer head screws with neoprene sealing washer, prepainted to match panels. Use 1/4” x 1-1/4” self-tapping screws with #1 size drilling point.

      - METAL WALL PANELS

        - General:  Provide factory-formed metal wall panels designed to be field assembled by overlapping and sealing seams, and attaching to wall structure with exposed screw fasteners.

        - Exposed fastener lap seam wall panels with sinusoidal corrugations at 2.67” on center.

- Throughout this article, select Cor-Pan 0.5 for nominal 1/2” deep corrugations or Cor-Pan 1.0 for nominal 1” deep corrugations.

          - Panel shall be IMETCO Cor-Pan [0.5] [1.0] panel system as manufactured by Innovative Metals Company, Inc. (IMETCO), Norcross, Georgia, telephone 1-800-646-3826.

          - Alternate manufacturers are subject to full compliance with specification requirements, and shall be submitted for approval as follows.

            - Manufacturers not listed above must submit for approval, ten (10) days prior vto bid date, the following:  Manufacturer's literature; certification of testing in accordance with specification requirements and sections 1.4 and 1.5; sample warranties in accordance with specification section 1.10; installer qualifications in accordance with specification section 1.6, and a list of five (5) similar projects in size and scope of work.

            - No substitutions will be permitted after the bid date of this project.

- Retain one of the following two paragraphs to specify the appropriate material type and sheet thickness for this project.

          - Material:  Zinc-coated (galvanized) steel sheet, [0.023-inch (0.56-mm)] [0.029-inch (0.71-mm)] [0.034-inch (0.86-mm)] nominal thickness.  See 2.1 for finishes and color selection.

          - Material:  Aluminum sheet, [0.032 inch (0.81 mm)] [0.040 inch (1.02 mm)] [0.050 inch (1.27 mm)] thick.  See 2.1 for finishes and color selection.

          - Characteristics.

            - Fabrication:  Panels shall be factory formed from specified metal.

            - The standard profile shall have sinusoidal corrugations at 2-2/3 inches (68 mm) on center.

            - Panel orientation: [Horizontal] [Vertical].

- The actual coverage width of Cor-Pan 0.5 is 40 inches; the actual coverage width of Cor-Pan 1.0 is 34-2/3 inches.

            - Configuration:  Panel shall be [40-inches- (1,016-mm-)] [34-2/3-inches- (880-mm-)] wide, nominal.

- The actual panel depth of Cor-Pan 0.5 is 1/2 inch; the actual panel depth of Cor-Pan 1.0 is 7/8 inch.

            - Panel Depth (Rib Height): [1/2 inch (13 mm)] [7/8 inch (22 mm)], nominal.

- Panel lengths in excess of 24 feet may be difficult to install on vertical wall applications. Consideration should be given to utilizing intermediate horizontal sill/head trim or panel end laps for these project conditions.

            - Panel length:  Up to 45 feet (13.7 m) maximum recommended length.

      - ACCESSORIES

        - Wall Panel Accessories:  Provide components approved by wall panel manufacturer and as required for a complete metal wall panel assembly including trim, copings, fasciae, corner units, head closures, cleats, flashings, sealants, gaskets, fillers, closure strips, and similar items.  Match material and finish of metal roof panels unless otherwise indicated.

          - Closure Strips:  Closed-cell, expanded, cellular, rubber or crosslinked, polyolefin-foam or closed-cell laminated polyethylene; minimum 1-inch- (25-mm-) thick, flexible closure strips meeting ASTM D1056 and/or D3575; premolded to match metal roof panel profile.  Provide closure strips at head (outside), sill (inside), and where necessary to ensure weathertight construction.

        - Flashing and Trim:  Formed from same material and gauge as wall panels, prepainted with coil coating.  Provide flashing and trim as required to seal against weather and to provide finished appearance.  Locations include, but are not limited to, head, sill, corners, jambs, framed openings, fasciae, and fillers.  Finish flashing and trim with same finish system as adjacent metal wall panels.

        - Gutters:  Formed from same material as wall panels.  Match profile of gable trim, complete with end pieces, outlet tubes, and other special pieces as required.  Fabricate in minimum 10-foot- (3-m-) long sections, of size and metal thickness according to SMACNA's "Architectural Sheet Metal Manual."  Furnish gutter supports spaced per SMACNA’s recommendation based on gauge and stretch-out, fabricated from same metal as gutters.  Provide wire ball strainers of compatible metal at outlets.  Finish gutters to match [metal wall panels] [metal roof panels] [roof fascia and rake trim].

          - Gutter Hangers:  External gutter supports shall be 2-inch- (50-mm-) wide x ¼-inch- (6-mm-) thick formed aluminum, and shall be spaced at no greater than 36” (0.9m) on center.  External supports shall be post-painted with a matching full-strength 70 percent PVDF finish and warranted by the panel manufacturer for same term as specified for material finishes.

          - Gutter Straps:  Internal gutter straps shall be 1-inch- (25-mm-) wide x 1/8-inch- (3-mm-) thick formed aluminum, and shall be spaced at no greater than 36” (0.9m) on center.  Internal straps shall be post-painted with a matching full-strength 70 percent PVDF finish and warranted by the panel manufacturer for same term as specified for material finishes.

        - Downspouts:  Formed from same material as wall panels.  Fabricate in 10-foot- (3-m-) long sections, complete with formed elbows and offsets, of size and metal thickness according to SMACNA's "Architectural Sheet Metal Manual".  Finish downspouts to match gutters.

          - Downspout Brackets:  Where detailed, surface mounted downspout protection guards shall be fabricated from ¼-inch- (6-mm-) thick formed aluminum, and shall be post-painted with a matching full-strength 70 percent PVDF finish and warranted by the panel manufacturer for same term as specified for material finishes.

      - FABRICATION

        - Fabricate and finish metal wall panels and accessories at the factory to greatest extent possible, by manufacturer's standard procedures and processes and as necessary to fulfill indicated performance requirements.  Comply with indicated profiles and with dimensional and structural requirements.

        - Provide panel profile, including major ribs and intermediate stiffening ribs, if any, for full length of panel.

        - Form flashing components from full single width sheet in minimum 10’-0” (3 m) sections.  Provide mitered trim corners, joined using closed end pop rivets and butyl-based, solvent released one-part sealant.

        - Sheet Metal Accessories:  Fabricate flashing and trim to comply with recommendations in SMACNA's "Architectural Sheet Metal Manual" that apply to the design, dimensions, metal, and other characteristics of item indicated.

          - Form exposed sheet metal accessories that are without excessive oil canning, buckling, and tool marks and that are true to line and levels indicated, with exposed edges folded back to form hems.

          - Sealed Joints:  Form nonexpanding but movable joints in metal to accommodate butyl-based sealant to comply with SMACNA standards.

          - Conceal fasteners and expansion provisions where possible.  Exposed fasteners are not allowed on faces of accessories exposed to view.

          - Fabricate cleats and attachment devices of size and metal thickness recommended by SMACNA's "Architectural Sheet Metal Manual" or by metal wall panel manufacturer for application, but not less than thickness of metal being secured.

      - FINISHES

        - Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes.

        - Protect mechanical and painted finishes on exposed surfaces from damage by applying a strippable, temporary protective covering before shipping.

        - Appearance of Finished Work:  Noticeable variations in same piece are not acceptable.  Variations in appearance of adjoining components are acceptable if they are within the range of approved Samples and are assembled or installed to minimize contrast.

- PREPERATION & EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for installation tolerances, metal wall panel supports, and other conditions affecting performance of the Work.

- Retain one or both of first two paragraphs below.

        - Examine primary and secondary wall framing to verify that girts, studs, angles, channels, and other structural panel support members and anchorages have been installed within alignment tolerances required by metal wall panel manufacturer.

        - Examine solid wall sheathing to verify that sheathing joints are supported by framing or blocking and that installation is within flatness tolerances required by metal wall panel manufacturer.

        - Examine roughing-in for components and systems penetrating metal wall panels to verify actual locations of penetrations relative to seam locations of metal wall panels before metal wall panel installation.

- Retain paragraph below if required.

        - For the record, prepare written report, endorsed by Installer, listing conditions detrimental to performance of the Work.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Clean substrates of substances harmful to insulation, including removing projections capable of interfering with insulation attachment.

- Retain first paragraph below if required to separate foam-plastic insulation from interior.

        - Substrate Board:  Install substrate boards over wall structure on entire wall surface.  Attach with substrate-board fasteners.

          - Install substrate board with long joints in continuous straight lines, horizontally oriented with end joints staggered between courses.  Tightly butt substrate boards together.

          - Comply with [UL] [FMG] requirements for fire-rated construction.

        - Miscellaneous Framing:  Install sub-framing, furring, and other miscellaneous wall panel support members and anchorage according to metal wall panel manufacturer's written instructions.

        - Establish straight, side and crosswise benchmarks

        - Use proper size and length fastener for strength requirements.

        - All walls shall be checked for square and straightness.  Inside and outside corners may not be plumb; set a true line for the corner flashing with string line.

        - Measure the wall lengthwise to confirm panel lengths and verify clearances for thermal movement.

      - THERMAL INSULATION INSTALLATION

        - Polyethylene Vapor Retarder:  Extend vapor retarder to extremities of areas to be protected from vapor transmission.  Repair tears or punctures immediately before concealment by other work.

        - Board Insulation (reference 2.2.C-G):  Extend insulation in thickness indicated to cover entire wall.  Comply with installation requirements in Division 07 Section "Thermal Insulation."

          - Erect insulation and hold in place with hat channels or Z-shaped furring.  Securely attach narrow flanges of furring members to wall framing with screws spaced 24 inches (610 mm) o.c.

      - UNDERLAYMENT INSTALLATION

        - Sheet Underlayment:  Apply primer if required by manufacturer.  Comply with temperature restrictions of underlayment manufacturer for installation.  Apply over entire wall surface, wrinkle free, in shingle fashion to shed water, and with end laps of not less than 6 inches (150 mm) staggered 24 inches (610 mm) between courses.  Overlap side edges not less than 3-1/2 inches (90 mm). Roll laps with roller.  Cover underlayment within 90 days.

      - METAL WALL PANEL INSTALLATION

        - All details will be shown on in accordance with approved shop drawings and manufacturer's product data, within specified erection tolerances.

- The specifier should customize this section to illustrate the intended scope of work for this project.

        - Directly over the completed wall substrate, install wall panels using specified exposed fasteners and sealants. Fastener spacing for anchorage to wall structure and stitching of lap seams shall be in accordance with manufacturer’s shop drawings and as required for structural strength and serviceability.

        - Installation of Wall Panels: Wall panels can be installed by starting from one end and working towards the opposite end. If panel end laps are approved by architect and shown on contract documents, installation shall be from bottom-to-top to allow for proper shingling effect of end laps.

        - Isolate dissimilar metals and masonry or concrete from metals with bituminous coating.  Use gasketed fasteners where required to prevent corrosive action between fastener, substrate, and panels.

        - Limit exposed trim and flashing fasteners to extent indicated on contract drawings.

        - Seal laps and joints in accordance with wall panel system manufacturer's product data.

        - Coordinate flashing and sheet metal work to provide weathertight conditions at wall terminations. Fabricate and install in accordance with standards of SMACNA Manual.

        - Provide for temperature expansion/contraction movement of panels at wall penetrations and wall mounted equipment in accordance with system manufacturer's product data and design calculations.

        - Installed system shall be true to line and plane and free of dents, and physical defects. In light gauge panels with wide flat surfaces, some oil canning may be present. Oil canning does not affect the finish or structural integrity of the panel and is therefore not cause for rejection.

        - At joints in linear sheet metal items, set sheet metal items in two ¼-inch- (6-mm-) beads of butyl sealant.  Extend sealant over all metal surfaces.  Mate components for positive seal.  Allow no sealant to migrate onto exposed surfaces.

        - Remove damaged work and replace with new, undamaged components.

        - Touch up exposed fasteners using paint furnished by the panel manufacturer and matching exposed panel surface finish.

        - Clean exposed surfaces of wall panels and accessories after completion of installation.  Leave in clean condition at date of substantial completion.  Touch up minor abrasions and scratches in finish.

      - ERECTION TOLERANCES

        - Installation Tolerances:  Shim and align metal wall panel units within installed tolerance of 1/4 inch in 20 feet (6 mm in 6 m) at location lines as indicated and within 1/8-inch (3-mm) offset of adjoining faces and of alignment of matching profiles.

      - FIELD QUALITY CONTROL

- Retain first paragraph below for assemblies requiring weathertight warranty.

        - Manufacturer's Field Service:  Engage a factory-authorized service representative to inspect metal wall panel installation, including accessories.  Report results in writing.

        - Remove and replace applications of metal wall panels where inspections indicate that they do not comply with specified requirements.

        - Additional inspections, at Contractor's expense, will be performed to determine compliance of replaced or additional work with specified requirements.

      - CLEANING

        - Remove temporary protective coverings and strippable films, if any, as metal wall panels are installed unless otherwise indicated in manufacturer's written installation instructions.  On completion of metal wall panel installation, clean finished surfaces as recommended by metal wall panel manufacturer.  Maintain in a clean condition during construction.

        - Replace metal wall panels that have been damaged or have deteriorated beyond successful repair by finish touchup or similar minor repair procedures.

END OF SECTION 074113